Product Description

PP-K4860 Which is produced by China Energy Group Ningxia Coal Industry Co., Ltd，based on NTH's Novolen gas-phase polypropylene technology.The product is produced with polymerized propylene and ethylene as the main raw material,Under the action of a catalyst,through the process of polymerization, separation, granulation, packaging, etc.

Product Specification

| No. | Testing item |  | Unit | PP-R,M,115-05-650(K4860) |
| --- | --- | --- | --- | --- |
| 1 | Particle appearance | Color granule | pcs/kg | ≤20 |
|  |  | Black granule | pcs/kg | 0 |
|  | 6 | Large granule and small granule | g/kg | Actual measurement |
| 2 | Melt mass-flow rate |  | g/10min | 65±10 |
| 3 | Total ash |  | mg/kg | Actual measurement |
| 4 | Yellow index |  |  | ≤0 |
| 5 | Tensile stress at yield |  | MPa | ≥22 |
| 6 | Flexural modulus |  | MPa | ≥800 |
| 7 | Charpy notched impact(23℃) |  | KJ/m2 | ≥2.8 |
| 9 | Rockwell hardness |  |  | Actual measurement |
| 9 | Temperature of deflection under load(Tf 0.45) |  | ℃ | Actual measurement |
| 10 | Haze |  | % | ≤20 |
| 11 | Moulding shrinkage | Parallel | % | Actual measurement |
|  |  | Vertical | % | Actual measurement |

Features	Applications

- High transparency	·Rapid injection molding

- High liquidity	·Milk Teacup

- Good processing performance	·Large thin-walled packaging containers