Polypropylene  PPB-M30(K8030)

Epoxidized Soybean Oil

Epoxidized Soybean Oil

Epoxidized Soybean Oil

Epoxidized Soybean Oil

TECHNICAL DATA SHEET

TECHNICAL DATA SHEET

TECHNICAL DATA SHEET

Polyvinyl Chloride Resin

Polypropylene PPB-M30

39021000

Product                                                                       TECHNICAL DATA SHEET

PP Co-polymer

HS code                                                                                                    PPB-M30

Oct 18th, 2020

Type

Print Date                                                     www.chemdo.com       info@chemdo.com

Description

Polypropylene, a kind of non-toxic,odorless, tasteless opalescent polymer with high crystallization, the melting point among 164-170℃, the density among 0.90-0.91g/cm3, the molecular weight is about 80,000-150,000. PP is one of the lightest plastic of all varieties at present, particularly stable in water, with a water absorption rate in water for 24 hours is only 0.01%.

Application Direction

The grade produced by the HORIZONE gas-phase polypropylene process of Japanese JPP company. It is mainly used for making washing machine internal and external parts, automotive interior parts, automotive modified materials and other products.

Product Packaging

In 25kg bag, 16MT in one 20fcl without pallet or 26-28MT in one 40HQ without pallet or 700kg jumbo bag, 26-28MT in one 40HQ without pallet.

Typical Characteristic

| ITEM | UNIT | INDEX | TEST METHOD |
| --- | --- | --- | --- |
| Melt mass flow(MFR) Standard value | g/10min | 30 | GB/T 3682.1-2018 |
| Melt mass flow(MFR) Deviation value | g/10min | ±4.0 | GB/T 3682.1-2018 |
| Tensile yield stress | Mpa | ≥ 22.0 | GB/T 1040.2-2006 |
| Flexural modulus(Ef) | Mpa | ≥ 1100 | GB/T 9341-2008 |
| Charpy notched impact strength (23℃) | KJ/m2 | ≥6.5 | GB/T 1043.1-2008 |
| Heat deflection temperature under load(Tf0.45) | ℃ | ≥ 90 | GB/T 1634.2-2019 |