TECHNICAL DATA SHEET

Description

400 Kt/a polyethylene unit adopts Hostalen slurry process of LyondellBasell Company and use ultra- high activity catalyst. The performance and stability of the product are ensured by adjusting the ratio of ethylene to comonomer in the circulating gas and the type of catalyst.

Application Direction

Mono-filaments made of Hostalen GF 7750 M2 exhibit excellent tensile strength and high elongation at break. Typical customer applications are ropes and yarns for nets, geotextiles and protective netting in agriculture and building industry.

Product Packaging

In 25kg bag, 26-28MT in one 40HQ

Typical Characteristic

| PROPERTIES | UNITS | TYPICAL VALUE | TEST METHOD |
| --- | --- | --- | --- |
| Density | g/m3 | 0.948 | GB/T1033.2-2010 |
| Melt Flow Rate(190℃/5kg) | g/10min | 0.25 | GB/T 3682.1-2018 |
| Tensile stress at yield | MPa | 22.1 | GB/T 1040.2-2006 |
| Tensile Elongation at Break | % | 807 | GB/T 1043.1-2008 |
| Charpy Impact Strength-Notched (23℃) | KJ/m2 | 33 | GB/T 9341 |
| Flexural modulus(Ef) | MPa | 1000 | GB/T 1040.2-2006 |
| Oxidation Induction Time(210℃,A1) | Min | 53.8 | GB/T 19466 |
| Rapid Crack Propagation(RCP, S4) | Bar | ≥10 | ISO 13477 |