DESCRIPTION FOR  
“CZ-502” SEMI-DULL PET CHIPS 

With increasing development of global economy and improvement of the people’s living standard, spinning & weaving industry, garment and beverage aspects as well as the various packing industry have been developed rapidly. The semi-dull PET (polyester) chips become main raw materials for further producing the textile fiber, and polyester industry film etc. with its characteristics of the excellent chromaticity, high intensity and good processing property.
“Sanfangxiang”Brand “CZ-502”semi-dull polyester chips are suitable for making the terylene filament & terylene staple fiber, PET industry film etc. This kind of semi dull chips possess the characteristics of meek tonality, uniform particle size, less impurity and stable viscosity. For applying the unique process recipe and production technology, the distribution of the chip’s molecular weight are centralized. So the chips are especially used to produce the fine denier filament and high-speed polyester film with the excellent further processing property, chromaticity performance, high rate of final products, less rate of fiber broken.
The company applied most advanced technology from DuPont, USA and all the equipments were imported abroad. The company always strictly organizes production and management based on the requirements stipulated in ISO 9001 Quality Guarantee System. The quality of “Sanfame” super-lustrous polyester chips is reliable and worthy to be trusted by all customers.

	“JADE” Brand “CZ-502” Semi-dull Polyester Chips

	Item
	Unit
	Index

	Viscosity
	dL/g
	0.655 ± 0.01

	Melting point
	℃
	259 ± 2

	Color value
	L
	-
	≥ 75

	
	b
	-
	4.0 ± 2.0

	Content of COOH
	mol/t
	28±4

	DEG Content
	wt%
	1.2 ± 0.15

	Agglomerated particles
	Pc/mg
	≤ 1.0

	Water content
	wt%
	≤ 0.4

	Powder content
	ppm
	≤ 100


